## Slide 1
Quarterly Case Study Session
Presented 2018
Water Containers and Plastic Waste
Claes Fredriksson and Bridget Ogwezi
Ansys Materials Education Division
Notes: Introduction
These Case Study Sessions are based on our Advanced Industrial Case Studies for Granta EduPack.
This is our fifth quarterly online training session for EduPack users, the topic is plastic waste, focusing on Sustainability and Eco Properties of water containers
These are intended to inspire educators, and facilitate materials-related teaching.

## Slide 2: Agenda
Introduction
Advanced Industrial Case Study
  Plastic Waste
  Useful Databases
  Level 2 vs Level 3
  Eco Audit of Water Containers
  Classroom Practical
Q&A
Community Update
Claes Fredriksson and Bridget Ogwezi
Ansys Education Team
Notes: Agenda
We will start with an introduction to the case study and give some background to the waste problem
Furthermore, we will discuss the content of our databases looking both at Level 3 and Level 2
Then we will be showing how you can use Granta EduPack to compare different water containers using an Eco Audit
This is an activity that can be performed in the classroom with some student participation

## Slide 3: Background: plastic waste
Enormous amounts of plastic litter today
Packaging problematic:
  Disposable plastics
  Drinks bottles etc
Up to 12 million tonnes/year plastics in the sea
  whole objects (on average 1 kg/km2)
  microplastic particles (1 million tonne/year primary)
  chemicals
Designers and Engineers must be aware of both pros and cons in materials decisions
Material properties causing problems:
  cheap/light
  not biodegradable
  very long expected life
Notes: Plastic waste background
Well over one million plastic bottles are bought around the world every minute and the number may have increased by up to 20% by 2021
Plastic bottles are likely to be floating, but only 1% of marine plastics are found near the surface of the ocean, with an average global concentration of around 1 kg/km2. The highest concentration is recorded in the North Pacific Gyre at 18 kg/km2.
Most plastic bottles used for soft drinks and water are made from polyethylene terephthalate (PET), which is highly recyclable. However, it is estimated that globally only around 9% of plastic waste is recycled.
Rather than to blame the material alone, we must look at the product design and how we use plastics in packaging.

## Slide 4: Materials data for design at Level 3
From the folder-level record
In specialized advanced editions
Notes: Level 3 data
There is plenty of materials data in Granta EduPack, covering a relevant range of materials for water containers; glass, aluminum, cardboard, and polymers, such as PET
In Level 3, there are so called folder-level records for each class of material, for example PET
This offers advanced design-guidance, such as strengths and limitations of the material class
Depending on which edition of Granta EduPack, there is additional data available
The Bioengineering database has food compatibility information
The Polymer database has large external databases from suppliers (Campus and Prospector Plastics) and around 200 chemical resistance properties
The Sustainability database has extra data-tables for Legislation and regulation about packaging, for example

## Slide 5: Level 3 has very specific information
The advanced databases have around 4000 material records
This enables very specific data
Use tiling on the top menu: Window
Notes: Level 3 strengths
The advanced databases have around 4000 material records, which enables very specific data
In the case of PET, there are two microstructurally different grades, amorphous (transparent) and semi-crystalline (opaque)
There are also a number of additional properties at Level 3 that are not found at Level 2
Mechanical properties, such as Rockwell hardness
More optical and thermal properties, for example thermal shock resistance and heat deflection temperatures.
There are also additional absorption and permeability attributes compared to Level 2...

## Slide 6: Level 2 vs Level 3
(compare: level 3 folder-level record)
Images for materials and processes
Good support for eco-design
Notes: Level 2 strengths
Although Level 3 has many more material records and more properties, Level 2 is relatively powerful for eco design
It has nice images, both of materials and their applications as well as manufacturing processes (e.g., blow molding)
It has rich support for design: design guidance, technical notes, environmental notes and typical uses

## Slide 7: Environmental/recycling data
Annual world production
Notes: Recycling
Resource data enables a plot of Annual world production. Here showing a subset: PE, PET, PP, PS, tpPVC,
A polymer that would be familiar to most people is a material used for plastic bottle caps, polypropylene (PP)
Although polypropylene is one of the most produced polymers in the world, a quick look at the Recycling and end of life information in the datasheet, seen below, reveals that there is less than 6% of recycled PP in the industrial supply
We can also see that PP is not biodegradable and at Level 2, all thermoplastics indicate recycling marks (See Science Note)).

## Slide 8: Virgin vs recycled materials
Notes: Energy and CO2 benefits of recycling
Here we can see that for all typical water container materials, the embodied energy is significantly lower for recycled material than for virgin
The trend is the same for the CO2 footprint, except for paper and cardboard, which are renewable (biological) materials
Recycled paper/cardboard is considered to have the same CO2 footprint, originating from transports and processing etc, as first cycle material.
The CO2 involved in the growth of the trees are sequestered from the air and growth is powered by the photosynthesis resulting in a very low footprint.

## Slide 9: What can Granta EduPack do?
Eco Audit tool for
Life-cycle investigations
CO2
Main players:
Notes: Eco Audit background
The Eco Audit tool in Granta EduPack can be used to compare different types water containers
For a fair comparison, the entire life-cycle of the product has to be considered (including transports)
With the Eco Audit, you can estimate energy use and CO2 emissions as well as see the effects of feedstock and recycling options
The Eco Audit is not a life-cycle assessment (LCA), but rather a streamlined life-cycle inventory (LCI)

## Slide 10: What can Granta EduPack do?
Life-cycle comparison of water containers by Eco Audit at Level 2 (data from 2018)
Container: | PET bottle (0.5 l) | PLA (0.5 l) | Al-can (0.33 l) | TetraPak (0.5 l)
Units for 10 litre [#] | 20 | 20 | 30 | 20
Material (bottle+cap) | PET+PP | PLA+PP | Wrought Al non-aged | Cardboard+PP
Mass [g] (bottle+cap) | 23+3 | 30+3 | 12.5 | 20+3
Mass [kg] (dummy) | 0.5 | 0.5 | 0.33 | 0.5
Recycled [%] | 21 | 0.3 | 42.5 | 71.9
Transport [km] | 405 | 188 | 936 (road)+41 (ship) | 1082 (road)+41 (ship)
Source | Armathwaite, UK | South Downs, UK | Perrier, France | Fläming, Germany
Energy [MJ] | 105 | 97 | 108 | 79
CO2 [kg/kg] | 5.53 | 6.11 | 6.95 | 4.22
Click to add text
Notes: Eco Audit Level 2
This selection represents a main PET bottle, as reference, and some options that can be compared and discussed in a life-cycle perspective, e.g., Polylactide (PLA) a biopolymer.
We have excluded glass bottles that can be cleaned and reused instead of recycled.
The masses were measured using baking scales with an accuracy limited to approximately +/- 0.5 g.
Actual distances for transport are entered, with information from the Internet concerning where the water has been sourced. For example Armathwaite (see first picture inset) to Cambridge in the UK: 404.5 km by road via A1 and A1 (M).
Don’t forget to add water.
The numerical values can be found within Detailed report, Otherwise, the Summary chart is convenient (next slide)

## Slide 11: Eco Audit comparison results
The use phase is represented by refrigeration for 2 whole days (static mode) using a UK electricity mix.
An average power use of 120 W is assumed here.
The use phase (refrigeration) is considerable
The Al can with typical recycled fraction (42.5%), has by far the largest material CO2 footprint
This can be changed by using 100% recycled Al
TetraPak has the lowest footprint (but is a hybrid)
Notes: Results
The use phase is represented by refrigeration for 2 whole days (static mode) using a UK electricity mix.
An average power use of 120 W is assumed in this example.
it is clear from this summary that the use phase (refrigeration) is considerable and that the Al can, using a recycled fraction taken from the typical industrial supply (42.5%), has a CO2 footprint for the material part twice that of any of the other options.
Overall, the Al can has the largest total energy use (18% higher than PET) and CO2 footprint (45% higher than PET). The TetraPak option has the lowest, 19% less energy and 10% lower CO2 footprint than PET.
It can also be seen that the transport phase may be significant, although both imported water containers (Al and TetraPak) have moderate relative energy consumption and emissions.
The manufacturing phase is relatively small for all containers.
These, or similar results that you generate yourselves, are open for interpretation and discussion in the classroom.

## Slide 12: Conclusions
Granta EduPack was helpful comparing PET bottles with alternative material options; PLA bottles, Al cans and TetraPak cartons.
Both level 2 and level 3 have useful data that can be employed to assess the containers, for example regarding recycled fraction in current supply of materials as well as embodied energy and CO2 footprint of virgin or recycled materials. This data provides a good platform for discussion in the classroom.
In the Eco Audit, the typical Al can had the highest footprint and the carton the lowest. You can easily explore the life-cycle impact of recycling, as demonstrated by changing the recycled fraction in the Al can feedstock, for instance. This highlights the consequences of materials decisions.
The combination of the software with a practical activity offers an engaging learning opportunity in the classroom.
Notes: Conclusions

## Slide 13: Practical classroom exercise
In the Case Study Paper:
The simple Eco Audit comparison is a suitable exercise to perform in small classes, as a practical lab for groups of 2-3 students. This has been tested with students of a European Winter School, during a session in Cambridge. All you need is digital scales of the type used for baking with a precision of about 0.5 g, or better. Containers can be contributed by the students or the educator and the results can be posted on the blackboard/ whiteboard in real-time during the session, in a table similar to the one we used. Glass bottles, soft waterbags or camping flasks for tap water can be used in the comparison. It can be interesting to compare the influence of different transport options, so try to find a diverse set of sources, domestic and exotic (Fiji, Canada, Switzerland, Italy, France etc, depending on your location) and research the distances and logistics involved.
Notes: Idea