## Slide 1
Unit 9.
Material and shape
Materials for efficient structures
Mike Ashby
Department of Engineering,
University of Cambridge
Notes: The PowerPoint Lecture Units For 2024
The Lecture Units developed for teaching in connection with Granta EduPack are listed at the end of this presentation.

## Slide 2: Learning objectives for this lecture unit
Intended Learning Outcomes | 
Knowledge and Understanding | Understanding of the concept of shape efficiency
Skills and Abilities | Ability to select efficient material-shape combinations
Values and Attitudes | Awareness of how materials and shape interact
Resources
Text: “Materials Selection in Mechanical Design”, 5th edition by M.F. Ashby, Butterworth Heinemann, Oxford, 2016, Chapters 10-11
Notes: Learning Objectives
These Intended Learning Outcomes are based on a taxonomy of knowledge and understanding as the basis, skills and abilities as necessary for the practical use of knowledge and understanding, followed by acquired values and attitudes enabling assessments and responsible use of these abilities.
Combined with a suitable assessment, they should be helpful in the context of accreditations or for the CDIO Syllabus.
The Texts listed are from books authored or co-authored by Mike Ashby but other texts are also referred to in the Science Notes.

## Slide 3: Outline of lecture unit 9
Efficient shapes: tubes, I-beams etc
The shape factor and shape limits
Material indices that include shape
Graphical ways of dealing with shape
The Ansys Granta EduPack Structural Sections data-table
Notes: Outline
This is the ninth Unit of a course on Material and Process Selection. The Units link closely to the Text listed on the previous frame but can equally by used in conjunction with texts such as Callister, Budinski, Askeland and others. The relevant chapters of the Texts are listed on the Outline frame of each Unit. The methods developed in the course are implemented in the Granta EduPack software, which is structured to evolve in pace with the student throughout a four-year engineering program. This first Unit introduces materials and processes, and the way in which information about them can be classified, stored, retrieved and explored.

## Slide 4: Shape efficiency
When materials are loaded in bending, in torsion, or are used as slender columns, section shape becomes important
”Shape” = cross section formed to a
        tubes
        I-sections tubes hollow box-section sandwich panels ribbed panels
“Efficient” = use least material for given stiffness or strength
Shapes to which a material can be formed are limited by the material itself
Goals: understand the limits to shape develop methods for co-selecting material and shape
Notes: Shape efficiency
In many applications section shape is not a variable. But when components carry bending, torsion or compressive loads, both the area and shape of the cross-section are important. By shape we mean that the cross-section is formed to a tube, I-section or the like. Efficient shapes use the least material to achieve a given stiffness or strength. It might seem that the way forward is to first choose the shape, then form the material into that shape. But some materials are routinely made into efficient shapes while are some or not, either because of manufacturing difficulties or because they buckle too easily (more on that later). So material and shape are coupled, requiring a method of choosing them together.

## Slide 5: Shape and mode of loading
Standard structural members
Area A matters,
not shape
Area A and shape IXX, IYY matter
Area A and shape J matter
Area A and shape Imin matter
Certain materials can be made to certain shapes: what is the best combination?
Tie
Beam
Torsion bar
Column
Notes: Loading
The choice of section shape is linked to the mode of loading. I-sections resist bending but are poor in torsion. Tubes resist torsion well. Tubes and box sections are good as columns, though I-sections are often used because their entire surface can be reached for painting and inspection, whereas the inner surface of tubes and boxes cannot.

## Slide 6: Shape efficiency: bending stiffness
Define shape factor for elastic bending, measuring efficiency, as
Take ratio of bending stiffness S of shaped section to that (So) of a neutral reference section of the same cross-section area
Define a standard reference section: a solid square with area A = b2
Second moment of area is I; stiffness scales as EI.
b
b
Area A is
constant
Area A = b2
Area A and modulus E unchanged
Notes: Bending
The obvious way to measure shape efficiency is to compare the behavior of a shaped section with that of a standard section with the same area – and thus the same mass of material per unit length. We take the standard section to be a solid square. If the square section is reshaped into a tube or I-section, the cross-section area stays the same but the bending stiffness increases. Bending stiffness is proportional to EI where E is Young’s modulus and I is the second moment of area of the cross section. The standard and the shaped beam are the same material, so E does not change. The second moment I increases from
I0 = A2/12
to I, so the bending stiffness increases by the factor
φe = I/I0 = 12 I/A2
The quantity φe measures the efficiency of the shape when stiffness is the goal. It is called the elastic shape factor.

## Slide 7: Properties of the shape factor
The shape factor is dimensionless – a pure number.
It characterizes shape.
Each of these is roughly 10 times stiffer in bending than a solid square section of the same cross-sectional area
Increasing size at constant shape
Circular tubes,
I-sections,
Notes: Shape factor
Area A has dimensions (m2) but shape φe , does not – it is a pure number. The frame shows I-sections and tubes with φe = 10, meaning that they are 10 times stiffer in bending than a solid square section of the same area. The three I-sections differ in size, but all have the same shape factor – each is a magnified version of the one on its left. The same is true of the tubes.

## Slide 8: Shape efficiency: bending strength
b
b
Define shape factor for onset of plasticity (failure), measuring efficiency, as
Area A is
constant
Take ratio of bending strength Ff of shaped section to that (Ff,o) of a neutral reference section of the same cross-section area
Section modulus of area is Z; strength scales as
Area A = b2
Area A and yield strength
unchanged
Notes: Bending
A parallel argument leads to the definition of the shape factor for the onset of yield or failure in bending. Here the act of shaping increases the section modulus Z. The efficiency is the ratio of this to the value
Z0 = A2/3/6
for the solid square section, giving the shape factor
φf = Z/Z0 = 6Z/A3/2
The quantity φf , the plastic shape factor, measures the efficiency of the shape when strength is the goal. Shapes with high φe have high φf as well. Similar shape factors characterize stiffness and strength in torsion.

## Slide 9: Tabulation of shape factors
Notes: Shape factors
The quantities I, Z and A can all be calculated from the dimensions of the section, allowing e φ to be calculated when these are known. This frame shows a small part of a larger table listing these (See “Materials Selection in Mechanical Design”). Note that the square section has a shape factor of 1; that for a solid circular section is very close to 1 (3/π = 0.95). That for thin wall tubes, box and I-sections is much larger.

## Slide 10: What values of e exist in reality?
Notes: Values of shape factors
Steel, aluminum, GFRP and timber are marketed as standard sections. There are a very large number of these. The figure on this frame shows I and A for about 1900 of them. Remember that the elastic shape factor is
φe = I/I0 = 12 I/A2
from which
I = φe A2/12
The scales are logarithmic, allowing φe to be shown as lines of slope 2. Two of these are shown, one for φe =1 and one for φe =100. Timber is available as square section beams (φe =1 ), but almost all other sections are more efficient than this. Few have an efficiency greater than about 65 – and none exceed 100 – it represents an upper limit for shape efficiency. A similar plot for Z and A allow the upper limiting values of φf to be explored. The picture is more complex than this. The only sections with φe > 45 are structural steel. The other materials have lower maximum shape factors. Each material has a different limit.

## Slide 11: Limits for shape factors e and f
Limit set by: (a) manufacturing constraints
(b) local buckling
Material Max e Max f
Steels 65 13
Aluminum alloys 44 10
GFRP and CFRP 39 9
Unreinforced polymers 12 5
Woods 8 3
Elastomers <6 -
Other materials ...can calculate
Theoretical limit:
Modulus
Yield strength
There is an upper limit to shape factor for each material
Notes: Limits of shape factors
The table lists empirical upper limits for shape factors for a number of materials. The limit is sometimes set by manufacturing constraints. But if these are overcome there is a practical upper limit related to the tendency of the section to buckle. Buckling is an unpredictable mode of failure, influenced by small geometric imperfections, and it can be catastrophic.
Yielding is benign – it gives warning. The more slender the structure the more easily it buckles. So the upper limit on slenderness and thus on φe , is set by the requirement that the structure yields before it buckles catastrophically, giving the equation shown on this frame.

## Slide 12: Indices that include shape
m = mass
A = area
L = length
 = density
b = edge length
S = stiffness
I = second moment of area
E = Youngs Modulus
Beam (shaped section).
Bending stiffness = S:
I is the second moment of area:
Chose materials with smallest
Function
Minimise mass, m, where:
Objective
Constraint
L
F
Area A
Notes: Derivation
The derivation here parallels that for a light stiff being given in Lecture Unit 7. The only difference is that, for the square beam of Lecture Unit 7
Io = A2/12
whereas for the shape beam
I = φe A2/12.
The resulting equation for the metric m shows how the mass of the beam depends on the mechanical constraint it must meet (S) on the section shape (φe ) and on the material of which it is made (ρ/E1/2). The quantity ρ /(φe E)1/2 can be thought as a “shaped-material index”.

## Slide 13: Selecting material-shape combinations
Material , Mg/m3 E, GPa e,max
1020 Steel 7.85 205 65 0.55 0.068
6061 T4 Al 2.70 70 44 0.32 0.049
GFRP 1.75 28 39 0.35 0.053
Wood (oak) 0.9 13 8 0.25 0.088
Materials for stiff, shaped beams of minimum weight
Fixed shape (e fixed): choose materials with low
Shape e a variable: choose materials with low
Commentary: Fixed shape (up to e = 8): wood is best
Maximum shape (e = e,max): Al-alloy is best
Steel recovers some performance through high e,max
Notes: Selection
The table shows an example of the comparison of materials for light stiff beams. When materials are compared with the same shape, it is sufficient to rank them by their value of ρ/E1/2. But when their shapes differ, they must be ranked by ρ/(φe E)1/2. The table shows that when these four materials are compared at constant shape (which must be less than φe =8 because timber is not available in more efficient shapes than this) then timber is the lightest. But if each material is shaped to its maximum value of φe , the lightest beam is that made of aluminum alloy; GFRP is close behind; and the steel beam is slightly lighter than the wooden one.

## Slide 14: Shape on selection charts
Al: e = 44
Al: e = 1
Note that New material with
Notes: Charts
The same comparison can be performed graphically – and this gives an interesting insight into the structural efficiency of wood. The shaped-material index can be re-expressed in terms of ρ* = ρ/φe and E* = E/ φe
The shape of the material can be thought of as a new material with “properties” ρ* and E* allowing it to be plotted on the E-ρ chart as shown here. The construction is shown here for aluminum, first as a solid square section when it lies at the values of ρ and E of aluminum, and second at the point (E/ φe, ρ/φe ).
A selection line for the index E1/2/ ρ is shown. Shaping has carried the aluminum across the line, into a region not occupied by an unshaped materials.

## Slide 15: Summary
When materials carry bending, torsion or axial compression, the section shape becomes important.
The “shape efficiency” is the amount of material needed to carry the load. It is measured by the shape factor, .
If two materials have the same shape, the standard indices for bending (e.g. ) guide the choice.
If materials can be made -- or are available -- in different shapes, then indices which include the shape (e.g. ) guide the choice.
Notes: Summary
The central idea here is that of shape efficiency and the ability to quantify it in a single set of dimensionless shape factors φe and φf . They measure the factor by which the shaped section is stiffer or stronger than one of a standard shape, which we take to be a solid square section of the same area. They allow the selection methods of the earlier Units to be adapted in a natural way to accommodate the selection of shaped materials.

## Slide 16: Lecture unit series
PowerPoint lecture units, as well as many other types of resources, can be found in the Ansys Education Resources webpage.
www.ansys.com/education-resources
Finding and Displaying Information | 
Unit 1 | The materials of engineering
Unit 2 | Material property charts: mapping materials
Unit 3 | The Elements database: properties, relationships and resources
Material Properties | 
Unit 4 | Manipulating properties: composition, microstructure, architecture
Unit 5 | Designing new materials: filling the materials-property space
Unit 6 | Materials Science and Engineering
Selection | 
Unit 7 | Material selection: translation, screening, ranking, documentation
Unit 8 | Objectives in conflict: trade off methods and penalty functions
Unit 9 | Material and shape: materials for efficient structures
Unit 10 | Manufacturing processes and cost modeling
Unit 11 | Eco-informed material selection
Unit 12 | Eco design and the Eco Audit tool
Sustainability
What is a sustainable development? A materials perspective
Exploring Critical Materials using Ansys Granta EduPack
Special Topics
The Built Environment: materials for construction
Structural sections: shape in action
Materials in industrial design: Why do consumers buy products?
The Design database for Products
The Medical Devices database
The Battery Designer tool
Advanced Teaching and Research
Advanced databases: a lightning tour
The Aerospace edition
The Polymer edition
The Synthesizer tool: hybrids and other models
Materials for Bioengineering
Notes: Lecture Units Series
This is a list of the Lecture Units available for teaching with the Ansys Granta EduPack. These PowerPoint presentations and more information can be found on the Ansys Education Resources webpage:
www.ansys.com/education-resources.